MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Mid Cool C600

A multi functional high performance EP water soluble metalworking fluid

Mid Cool C600 is a high performance water-soluble coolant designed for moderate to heavy duty machining operations. It is compatible with a wide range of metals and water hardnesses.

Mid Cool C600 has been developed as a high performance low foaming coolant for moderate to difficult machining operations on ferrous, non-ferrous and other high performance alloys.

Mid Cool C600 incorporates the latest performance additives including extreme pressure; the product also exhibits excellent lubricity characteristics to provide both good tool life and surface finish. The product is highly resistant to bacteria formation and exhibits excellent corrosion resistance whilst maintaining machine cleanliness and operator acceptability.

Application & Benefits

 Reaming

 Tapping and threading

 Deep hole drilling and boring

 Sawing

 Milling

 Heavy Duty Turning & Broaching

 Metal Forming

 Contains high EP & lubricity additives

 Low foam at high pressure

 Suitable on ferrous, non ferrous, and high performance alloys

 Suitable for use in hard and soft water

 High performance in arduous operations

 Excellent finish especially on non ferrous materials

| Typical Operations |  |  |  |
| --- | --- | --- | --- |
|  Drilling | 4% to 8% |  General machining | 4% to 6% |
|  Reaming | 8% to 12% |  Boring | 8% to 12% |
|  Threading,tapping | 5% to 10% |  Metal forming | 4% to 12% |
|  Broaching, sawing | 8% to 10% |  Turning, milling | 4% to 6% |

| Mid Cool C600 |  |  |  |
| --- | --- | --- | --- |
| Characteristics | Typical Data | Characteristics | Typical Data |
| Appearance | Amber liquid | IP287 corrosion breakpoint | 3% (v/v) |
| Odour | Bland | Specific Gravity (@20oC) | 0.97 |
| Emulsion Appearance | Milky Beige | Loadbearing capacity (kg/mm2) | 2.250 |
| PH (@ 5% concentration) | 9.5 | Refractometer Conversion Factor |  |

Mid Cool is a truly versatile water soluble metalworking fluid that can be used across a diverse range of metals, applications and water hardnesses. The performance parameters of Varcool 3010 make it an ideal candidate product to be used throughout a machine shop as a high performance general purpose coolant and metal forming fluid . Consideration should be given to the composition of materials if being used on sensitive aerospace alloys and there final use in flying rotating parts, if required please consult your local selling agent or Varol Technical Department for further information.

Bio-stability - these products give excellent bio-control maintaining bacteria levels well within the HSE (Health and Safety Executive) guidelines.

Corrosion inhibition - These products give equivalent corrosion protection, or better than boron containing products.

Operational Recommendations

Mid Cool C600 is designed to be mixed with water; it has been developed to exhibit full multi-metal compatibility and is suitable for use in soft and hard water types.

Mix emulsions of Mid Cool C600 with water by adding concentrate to water and then mixing or use a suitable proportioning mixer unit, these are available on request. The use of an airline to mix the solution is not recommended. Machine top up may require a weaker dilution than the initial machine charge concentration. Recommended concentrations can vary depending on operations, materials, tooling, coolant pressure, coolant flow. The above information is given for guidance. Please contact your representative for further advice.

Mid Cool C600 should always be stored indoors and protected from frost. Good standards of hygiene and housekeeping should always be adopted when using any metalworking fluid. A separate MSDS is available for this product.

As with all modern cutting fluids, concentration control is of paramount importance, therefore regular check by use of a refractometer is recommended for this product. It should be noted that the individual product refractometer correction factor should always be used to ensure accuracy.