MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Mid Form 149

A Low viscosity chlorinated neat oil for drawing, stamping and forming.

Mid Form 149 is a light coloured neat drawing, stamping or forming compound. It has low to medium viscosity and is suitable for many applications and a wide range of alloys including Steel, Stainless Steel and non ferrous metals.

Mid Form 149 is been developed and formulated with high levels of extreme pressure and lubricity additives in a highly refined mineral oil base.

Mid Form 149 is designed for use on a broad range of alloys and has superior EP and lubricity and is highly recommended for Stamping, Drawing, Blanking, Roll forming and other Cold head operations.

Application & Benefits

 Drawing and Stamping

 Fine Blanking

 Swaging

 Cold Heading and Roll Forming

 High EP and Lubricity properties

 Low viscosity so can be applied by Spray, Roller or Dip methods

 Spreads easily and evenly to cover the complete surface of the blank

 Completely Stable

 Suitable for non Ferrous metals and alloys including Steel, Stainless Steel

| Mid Form 149 |  |  |  |
| --- | --- | --- | --- |
| Characteristics | Typical Data | Characteristics | Typical Data |
| Appearance | Light Brown | Viscosity (@40oC) | 25 mm2/s |
| Chlorine | Yes | Specific Gravity (@20oC) | 0.97 |
| Ester | Yes | Loadbearing capacity (kg/mm2) | N/A |
| Sulphur | No | Refractometer Conversion Factor | N/A |

Mid Form 149 is designed to be used as supplied and can be applied by brush, roller or spray.

Mid Form 149 Parts formed with Mid Form 159 can be cleaned with caustic, alkaline or solvent cleaners. Parts should be cleaned before welding or any heat treatment operations take place.supplied s designed to be used as supplied and can be applied by brush, roller or spray.

Bio-stability - these products give excellent bio-control maintaining bacteria levels well within the HSE (Health and Safety Executive) guidelines.

Operational Recommendations

Mid Form 149 should always be stored indoors and protected from frost. Good standards of hygiene and housekeeping should always be adopted when using any metalworking fluid. A separate MSDS is available for this product.

As with all modern cutting fluids, concentration control is of paramount importance, therefore regular check by use of a refractometer is recommended for this product. It should be noted that the individual product refractometer correction factor should always be used to ensure accuracy.