MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Mid Form 180

A medium high viscosity chlorinated neat oil for drawing, stamping and forming.

Mid Form 180 is a light coloured medium viscosity drawing compound designed for arduous applications such as deep drawing of steels and heavy duty pressings or stamping operations.

Mid Form 180 is formulated with high levels of extreme pressure and lubricity additives in a highly refined mineral oil base. It includes additives to assist in the removal of residue.

Mid Form 180 is designed for use on mild and alloy steels, additionally it is a non staining towards Yellow metals making it also suitable for materials such as Copper or Brass.

Application & Benefits

 Deep Drawing and Stamping

 Fine Blanking

 Tube Forming and Drawing

 Very high EP and Lubricity properties

 Can be applied by Spray, Roller or Dip methods

 Based on highly refined mineral oils

 Completely Stable

 Medium viscosity making it easy to apply

| Mid Form 180 |  |  |  |
| --- | --- | --- | --- |
| Characteristics | Typical Data | Characteristics | Typical Data |
| Appearance | Light Brown | Viscosity (@40oC) | 35 mm2/s |
| Chlorine | Yes | Specific Gravity (@20oC) | 1.1 |
| Ester | Yes | Loadbearing capacity (kg/mm2) | N/A |
| Sulphur | No | Refractometer Conversion Factor | N/A |

Mid Form 180 is designed to be used as supplied and can be applied by brush, roller or spray.

Mid Form 180 Parts formed with Mid Form 180 can be cleaned with caustic, alkaline or solvent cleaners. Parts should be cleaned before welding or any heat treatment operations take place.supplied s designed to be used as supplied and can be applied by brush, roller or spray.

Operational Recommendations

Mid Form 180 should always be stored indoors and protected from frost. Good standards of hygiene and housekeeping should always be adopted when using any metalworking fluid. A separate MSDS is available for this product.

As with all modern cutting fluids, concentration control is of paramount importance, therefore regular check by use of a refractometer is recommended for this product. It should be noted that the individual product refractometer correction factor should always be used to ensure accuracy.