MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

15w/40 E3 E5 SHPD - Marine

Product Description – Super High Performance

Midlands Lubricants 15W/40 is a super high performance marine diesel multi-grade engine oil formulated to meet API SL/CH-4 and ACEA A3/B3, E5 performance requirements for use in turbo-charged and naturally aspirated petrol and diesel fuelled engines. With a total base number (TBN) of 15 it is highly recommended for marine engines, including trunk piston engines.

###### FEATURES/BENEFITS:

Excellent High and Low Temperature Performance
Long-Lasting Dispersant delivers a High Standard of Engine Cleanliness
Good Protection against Ring Sticking at High Temperatures
Maintains Oil Performance with Low Oil Consumption and Emissions
Excellent Sludge Control – prevents black sludge formation
Anti-Wear and Corrosion Protection
Extended Drain and Long Life Service

###### PERFORMANCE PROFILE:

API: SL/CH-4
ACEA: A3/B3, E3, E5
MB: 228.3, 229.1
Volvo: VDS-3
Cummins: 20071/72/76/77
VW: 500.01, 505.00
MAN: M3275
Renault: RVI RLD

Typical Properties:

Total Base Number (TBN)     15 mgKOH.g-1

Density, g.cm-3 @ 15.5°C      0.890			Kinematic, 40°C     110 cSt

Flash Point, COC         225°C				Kinematic, 100°C    14.9 cSt

Pour Point -27°C					Sulphated Ash       1.30% wt

Viscosity Index 150