MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

10w/40 SUTO Semi Synthetic SL/CG-4

Product Description

10w/40 Super Universal Tractor Oil (SUTO) is an high quality semi synthetic super universal performance engine oil that meets all the lubrication requirements of farm tractors and agricultural machinery. SUTO is an multi grade viscosity oil that covers a wide temperature range and is highly recommended for use in a variety of engines including naturally aspirated and turbocharged diesel and petrol engines. It is suitable for use in tractor hydraulic, transmission, and wet brake systems as well as gear boxes in farm machinery.

10w/40 SUTO provides excellent protection under the most arduous operating conditions and is formulated according to the most demanding performance requirements. 10w/40 Semi Synthetic SUTO includes friction modifier additives to provide smooth operation of the wet brake system to prevent squawk and chatter. 10w/40 SUTO offers the convenience of a single lubricant approach that delivers top performance and avoids the need for stocking of multiple lubricants.

Features/Benefits:

Excellent thermal stability & Reduced Friction / Fuel consumption

Low drag formulation / Low Chlorine formulation / Low Oil consumption

Excellent Engine cleanliness and resistance to black sludge

Low emissions with rapid circulation on start up and excellent anti wear

Performance/Specifications:

10w/40 Super Universal Tractor Oil meets a comprehensive range of international performance and specification requirements including:

Case: MS 1206

John Deere: JD 303, JD20A, J14B, JD20C

Ford: M2C134D, M2C159B, ESN-86A/B

Massey-Ferguson: M1135, M1144, M1145, M1127A, M1139A,

New Holland: NH 410B – Valtra G2-98

API: GL4   = SL/CG-4

MIL-L2104C/D, MIL-L45199B, MIL-L-2105

Caterpillar: Series 3

IH B6

Typical Properties:

Density, g.cm-3 @ 15°C 0.893

TBN = 10.3 mgKOH/g

Flash Point, COC 220°C

Pour Point -30°C

Sulphated Ash = 1.17%

Viscosity

Kinematic, 40°C = 86 cSt

Kinematic, 100°C = 11.2 cSt

Viscosity Index 128

These data are typical of current production, and whilst future production will meet these specifications, some variation in typical data may occur.