MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Heat Transfer Oil

MIDTRANS Heat Transfer Oils

Midlands Lubricants Heat Transfer Oils (HTO) are high quality heat transfer fluids based on highly refined mineral oils. Our MidTrans HTO oils are suitable for use in heat transfer systems requiring a heat transfer fluid in the liquid phase. In operating systems the product will perform within temperature ranges between -5°C and 360°C.

Applications & Benefits

Systems between –5 and 360°C

High quality solvent refined mineral Oil with low aromatic content

Good stability with low vapour pressure

Long life oxidation resistance

Excellent heat transfer properties

| Typical Properties ISO Grade |  |  |  |  | 22 | 32 |  | 46 | 68 | 100 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Kinematic Viscosity |  |  |  |  |  |  |  |  |  |  |  |
| at 40°C, cSt |  |  |  |  | 19.8 | 31.5 |  | 45.9 | 68.6 | 99.6 | Mm2/s |
| Viscosity Index |  |  |  |  | 95 | 95 |  | 95 | 95 | 95 |  |
| Flash Point, COC, °C |  |  |  |  | 198 | 200 |  | 205 | 210 | 220 |  |
| Pour Point, °C |  |  |  |  | -9 | -6 |  | -6 | -6 | -6 |  |
| Density, g.ml-1 |  |  |  |  | 0.868 | 0.87 |  | 0.87 | 0.87 | 0.878 | at 20°C |
| Carbon Residue 0.05 |  |  |  |  |  |  |  |  |  |  |  |

Operational Recommendations

Midland Lubricants MidTrans Heat Transfer Oil (HTO oils) are normally used as supplied.

HTO oils should always be stored indoors and protected from extremes of temperature. Good standards of hygiene and housekeeping should always be adopted when using any industrial oils.

A separate MSDS is available for this product.