MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

AFT Dexron VI

Product Description

Midlands Lubricants Full synthetic ATF fluid with advanced additive technologies to cover multi vehicle OEMs. Blended for high efficiency and fuel economy with low viscosity.

FEATURES / BENEFITS

Excellent frictional stability Anti-shudder & anti-wear properties Suitable for automatic transmissions and power steering systems for many European, American and Asian vehicles.

PERFORMANCE / SPECIFICATIONS

- GM Dexron VI

- Aisin Warner AW-1

- Honda DW-1

- Hyundai/Kia SP-IV, SPH-IV, SP-IV RR, NWS-9638

- JASO 1-A-LV

- JWS 3324 Mitsubishi ATF-J2, SP-IV

- Nissan Matic S

- Toyota WS (JWS 3324)

- Audi G 055 005, G 055 162, G 060 162 A2

- BMW 83 22 0 142 516, 83 22 2 152 426

- MB 236.12, 236.14, 236.15

- Saab 93 165 147

- VW G 055 540 A2, G 055 005, G 055 162, G 060 162 A2

TYPICAL PROPERTIES

- Colour Red

- Density, g.ml-3 @ 15°C = 0.851

- Flash Point, COC = 237°C

- Pour Point = -51°C

- Viscosity Kinematic @ 40°C = 29 cSt