MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

5w/30 C3 – Full Synthetic Engine Oil

Product Description

Midlands Lubricants Fully Synthetic 5W/30 C3 engine oil is produced from high quality synthetic base oils and top-tier performance additives.

FEATURES / BENEFITS

Suitable for use in petrol and diesel engines requiring VW specified lubricant performance. Blended to ensure fuel efficiency, reduced wear and low emissions. Low SAPS technology delivers a high level of engine cleanliness and protection from combustion contamination. Provides optimum performance and engine protection at temperature. Also recommended for vehicles 2004-2008 requiring A3,B3,B4

PERFORMANCE / SPECIFICATIONS

- API: SN/CF

- ACEA:C3-12

- BMW: Longlife-04  - VW 502: 505/505.01

- GM: Dexos 2 (formerly GM GEOS)

- MB: 229.31, 229.51 & 229.52

TYPICAL PROPERTIES

- TBN, mgKOH.g-1 = 7.5

- Density, g/cm3 @ 15°C = 0.856

- Flash Point, COC = 220°C

- Pour Point -40°C

- Viscosity Kinematic, @ 40°C = 67 cSt

- Kinematic, @ 100°C = 11.5 cSt

- Viscosity Index 167