MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

5w/30 – Full Synthetic Engine Oil suitable for LL-01 & 913B

Product Description

Midlands Lubricants super Fully Synthetic 5W/30 multi grade engine oil is produced from high quality synthetic base oils and top-tier performance additives. Our 5w/30 Fully Synthetic Engine Oil covers BMW LL-01 and is produced for excellent performance as well and fuel economy.

FEATURES / BENEFITS

Excellent High and Low Temperature Performance
Long-Lasting Dispersant delivers a High Standard of Engine Cleanliness
Good Protection against Ring Sticking at High Temperatures
Maintains Oil Performance with Low Oil Consumption and Emissions
Excellent Sludge Control Designed for Stop-Go City Motoring
Anti-Wear and Corrosion Protection
Reduced oil consumption and emissions

PERFORMANCE / SPECIFICATIONS

- API: SN/CF

- ACEA: A1-12/ B1-12

- BMW: Longlife-01

- ILSAC: GF-3

- Ford: WSS-MC2 913A - WSS-MC2 913B

TYPICAL PROPERTIES

- TBN, mgKOH.g-1 = No data

- Density, g/cm3 @ 15°C = 0.880

- Flash Point, COC = 208°C

- Pour Point =  -40°C

- Viscosity Kinematic, @ 40°C = 64 cSt

- Kinematic, @ 100°C = 10.8 cSt

- Viscosity Index 137