MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

PRODUCT NAME :  HVI Hydraulic Oils                            	        PRODUCT CODE :

Midlands Lubricants provides a comprehensive range of high quality High Viscosity Index (HVI) hydraulic oils suitable for use over a wide range of operating temperatures. HVI hydraulic oils are made from solvent refined base oils incorporating high performance hydraulic oil additives to provide excellent protection against oxidation, corrosion, wear and foaming and are boosted by the addition of polymeric viscosity index improver additives that enable these oils to maintain an effective lubrication viscosity at elevated temperatures

FEATURES   - Blended new virgin oil – Excellent Cleanliness filtration 4 microns pure

- Excellent High and Low Temperature performance

- 6743/4 category HV – Vickers M-2950-S & I-286-S

- Meets the anti-wear requirements of DIN 51524 part 3 - HVLP

| HVI ISO Grade | HVI 15 | HVI 22 | HVI 32 | HVI 46 | HVI 68 | HVI 100 |
| --- | --- | --- | --- | --- | --- | --- |
| Classification HV |  |  |  |  |  |  |
| Density, g.ml-1 | 0.87 | 0.872 | 0.876 | 0.876 | 0.878 | 0.88 |
| Kinematic Viscosity |  |  |  |  |  |  |
| ...at 0°C, cSt | 160 | 210 | 280 | 550 | 925 | 1730 |
| ...at 20°C, cSt | 39 | 55 | 80 | 128 | 200 | 340 |
| at 40°C, cSt | 15 | 22 | 32 | 46 | 68 | 100 |
| at 100°C, cSt | 3.6 | 4.6 | 6.5 | 8.4 | 10.9 | 13.9 |
| Viscosity Index | 154 | 155 | 155 | 156 | 157 | 158 |
| Flash Point, COC, °C | 178 | 185 | 205 | 212 | 218 | 226 |
| Pour Point, °C | -36 | -34 | -33 | -33 | -33 | -32 |
| ASTM D1401: Demulse, mins | 5 | 10 | 10 | 15 | 15 | 20 |
| IP 153B: |  |  |  |  |  |  |
| Salt Water Corrosion | Pass | Pass | Pass | Pass | Pass | Pass |
| IP 313: ARV 50°C, 0.2% air | 5 | 7 | 8 | 8 | 9 | 12 |
| IP154: Copper Corrosion | Pass | Pass | Pass | Pass | Pass | Pass |
| Rating 1 DIN 51389: |  |  |  |  |  |  |
| Vickers Vane Pump, |  |  | Less than | 50mg |  |  |
| IP 146: |  |  |  |  |  |  |
| Sequence I | 20/0 | 20/0 | 20/0 | 30/0 | 40/0 | 40/0 |
| Sequence I | 10/0 | 10/0 | 10/0 | 10/0 | 20/0 | 30/0 |
| Sequence I | 20/0 | 20/0 | 20/0 | 20/0 | 40/0 | 40/0 |
| IP 278: Seal Copatibility | 10.5 | 10.5 | 10.3 | 9.2 | 7.4 | 5.2 |