MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

15w/40 E9 SN/CK-4 CJ-4

Product Description

Midlands Lubricants 15W/40 E9 SN/CK-4 CJ-4 is a top-tier mixed-fleet multi-grade engine oil suitable for use in the latest heavy duty diesel and petrol engines. 15W/40 E9 SN/CK-4 CJ-4 meets the latest ACEA and API performance levels and is formulated for use in EuroVI technology vehicles where low SAPS levels are specified. Ultra High Performance Diesel (UHPD)

###### FEATURES/BENEFITS:

Low Saps Technology

Wide Ranging Fleet Product for Diesel and Petrol Engines
Excellent Protection for European, US and Japanese Engines.
Protects against Wear and Ring Sticking at High Temperatures, maintaining Engine and Oil Performance.
Low Oil Consumption and Extended Oil Drain Intervals
Excellent High and Low Temperature Performance
Long Lasting Dispersant, Anti-wear and Corrosion Protection

###### PERFORMANCE PROFILE: 15w/40 E9 SN/CJ4 meets the performance requirements of:

API SN/CK-4 CJ-4				Scania – Low Ash
ACEA: E7, E9 E11				VW: 505.00 Quality 
Cummins: CES 20086 Approved		Detriot Diesel 93K222 Approved
Mack: EOS 4.5 Approved			CAT: ECF-2, ECF-3
MB: 228.31 Approved			Deutz: DQC III-10-LA Approved
VW: 505.00 quality				MTU DDC Type 2.1 Approved
Volvo: VDS-4.5 Approved			MAN: M3775 Approved & M3575
RVI: RLD3 Approved & RLD 4		Ford: M2C171-F1 Approved
Typical Properties:

Total Base Number (TBN)     12 mgKOH.g-1

Density, g.cm-3 @ 15.5°C      0.888			Kinematic, 40°C     115 cSt

Flash Point, COC         218°C				Kinematic, 100°C    15.4 cSt

Pour Point -38°C

Viscosity Index 143